## Slide 1: Polymer Physics: Theory & Simulation
Angelo Rosa
SISSA-Trieste, June 2019
Email: anrosa@sissa.it

## Slide 2: Outline
Part I - Introduction to Polymers
Part II - Polymer Physics
  Structure
  Dynamics
Part III - Simulations methods:
  Exact enumeration
  Monte Carlo
  Molecular Dynamics

## Slide 3: History of Polymer Science
Materials: Stone Bronze Iron Plastics
Macromolecular synthesis from the middle of the 19th century
Macromolecular hypothesis (1920’s), H. Staudinger (Nobel Prize Chem., 1953)
U. W. Suter, Why Was the Macromolecular Hypothesis Such a Big Deal?
Adv. Polym. Sci. 261, 61 (2013)
Definition:
Polymers (from Greek, poly=“many” + meros=“parts”) are chain molecules consisting of 102-109 monomeric units joined together by chemical reaction
Statistical polymer physics:
Basic ideas (1930-60): Kuhn, Flory, Huggins, Stockmayer, James, Guth, Zimm, Rouse
Correlations / entanglements (1960-90): Edwards, de Gennes, des Cloizeaux

## Slide 4: Chain reaction
Polymerization, process of covalent bonding of elementary units:
R = H => Polyethylene
R = Cl => Polyvinylchloride (PVC)
R = Benzene => Polystyrene

## Slide 5: Polymer architectures

## Slide 6: Biopolymers
Proteins
Nucleic acids: DNA, RNA
Chromatin

## Slide 7: Polymers, main features
a) Chain connectivity
b) Aggregate states / dilution
1. Gas: dilute solutions
2. Liquid: semi-dilute solutions / melts
  3. Solid: rubber-elastic networks, polymer glasses, semi-crystalline polymers
Polyethylene
Polystyrene

## Slide 8: Polymers, main features
c) The effect of chain length, properties of the alkane/PE series:
Solution/melt:
Low molecular weight High molecular weight
No entanglement Yes entanglement

## Slide 9: Scale invariance: Polymers are fractal objects

## Slide 10: Scale invariance: Polymers are fractal objects

## Slide 11: Scale invariance: Polymers are fractal objects

## Slide 12: Scale invariance: Polymers are fractal objects
Every sub-chain behaves as the whole chain
Ça va sans dire, corresponding end-to-end distribution functions have also the same functional form (Gaussian, Redner-Des Cloizeaux, …) -> The concept of universality!

## Slide 13: Outline
Part I - Introduction to Polymers
Part II - Polymer Physics
  Structure
  Dynamics
Part III - Simulations methods:
  Exact enumeration
  Monte Carlo
  Molecular Dynamics

## Slide 14: Linear polymers

## Slide 15: Linear polymers
Bouchaud & Georges
PRB (1989)

## Slide 16: Linear polymers: g>1, n=1/2 =>
qi
qi+2
Freely-jointed chain: (qi, fi) unrestricted
qi+1
fi
Freely-rotating chain: (qi=q, fi unrestricted)
qi=q
qi+1=q
fi+1
fi

## Slide 17: Linear polymers: g>1, n=1/2 =>
Kuhn’s model:
qi
qi+2
qi+1
fi
qi=q
qi+1=q
fi+1
fi

## Slide 18: Linear polymers: g<1, n=(2-g)/2 =>
Excluded volume:
Two monomers can not occupy the same position in space!
PJ Flory

## Slide 19: Outline
Part I - Introduction to Polymers
Part II - Polymer Physics
  Structure
  Dynamics
Part III - Simulations methods:
  Exact enumeration
  Monte Carlo
  Molecular Dynamics

## Slide 20: Polymers dynamics: The Rouse-Zimm Model
Theoretical foundations: The Brownian motion
  Consider a system of `large’, freely diffusing particles (red) in a homogeneous medium composed of smaller particles (blue);
  The red particles collide randomly with the blue particles;
  Due to random collisions, the motion of red particles is erratic as well
  After time t, red particles have traveled – on average – a distance dr2(t)

## Slide 21: Polymers dynamics: The Rouse-Zimm Model
Polymer chain: the red particles are now linearly connected
  How does this affect the time behavior of the mean-square-displacement dr2(t)?

## Slide 22: Polymers dynamics: The Rouse-Zimm Model
Polymer chain: the red particles are now linearly connected
  How does this affect the time behavior of the mean-square-displacement dr2(t)?
  Clearly, at very short times, each monomer moves does not “feel” the presence of the other monomers -> dr2(t) = 6Dt

## Slide 23: Polymers dynamics: The Rouse-Zimm Model
Polymer chain: the red particles are now linearly connected
  How does this affect the time behavior of the mean-square-displacement dr2(t)?
  Clearly, at very short times, each monomer moves does not “feel” the presence of the other monomers -> dr2(t) = 6Dt
  At later times ?? More and more monomers become involved !!

## Slide 24: Polymers dynamics: The Rouse-Zimm Model
Linear connectivity + Gaussian fluctuations => elastic springs
“microscopic” time-scale
relaxation of subchains of length “N/p”

## Slide 25: Polymers dynamics: Viscoelasticity
Example: Silly Putty©
Silly Putty© is marketed today as a toy for children, but was originally created by accident during research into potential rubber substitutes for use by the United States in World War II.
Silly Putty©:
  bounces;
  breaks when given a sharp blow;
  can also flow like a liquid.
Silly Putty©'s unusual flow characteristics are due to the ingredient polydimethylsiloxane (PDMS), a viscoelastic liquid.
Viscoelasticity is a type of non-Newtonian flow, characterizing material that acts as a viscous liquid over a long time period but as an elastic solid over a short time period.
Source: Wikipedia

## Slide 26: Outline
Part I - Introduction to Polymers
Part II - Polymer Physics
  Structure
  Dynamics
Part III - Simulations methods:
  Exact enumeration
  Monte Carlo
  Molecular Dynamics

## Slide 27: Simulation methods. 1: Exact enumeration
Example: self-avoiding-walks vs. random-walks on the 2d simple cubic lattice
N=3

## Slide 28: Simulation methods. 1: Exact enumeration
Example: self-avoiding-walks vs. random-walks on the 2d simple cubic lattice
Schram et al., J Stat Mech (2011) P06019
m: non universal, depends on lattice choice
n, q: universal

## Slide 29: Simulation methods. 2: Monte Carlo
Problem: Numerical evaluation of p=3.1415926535…
+
+
+
+
+

## Slide 30: Simulation methods. 2: Monte Carlo
In practice, MC means to sample the space of configurations with the “correct” probability. In this case, the uniform distribution on the 2d circle:
Ntot=100
Ntot=1’000
Ntot=10’000
Ntot=100’000
Ntot=1’000’000
Ntot=10’000’000
The black line corresponds to the exact expression

## Slide 31: Simulation methods. 2: Monte Carlo
Alan D. Sokal, “Monte Carlo methods for the self-avoiding walk”, http://arxiv.org/abs/hep-lat/9509032

## Slide 32: Simulation methods. 3: Molecular Dynamics
Numerical solution of Newton’s equations for a system of N particles (coupled to each other):

## Slide 33: Simulation methods. 3: Molecular Dynamics
How to impose:
a) Excluded volume
b) Connectivity
Kremer & Grest, JCP 92 (1990)

## Slide 34: Simulation methods. 3: Molecular Dynamics
Exercise:
  Impose linear connectivity to a certain number of monomers (say, 10-20)
  Check distances between n.n. monomers (should remain close to s)
  Simulate a single polymer chain WITHOUT and WITH “solvent”
  Equilibrate the chain, monitor:
    g1(t) := single-monomer time mean-square-displacement (msd)
    g2(t) := single-monomer time msd in the frame of the polymer
    g3(t) := time msd of the center-of-mass of the polymer
  In particular, study single-monomer time msd (g1(t)):
    WITHOUT => Rouse
    WITH => Zimm